Mini project

We are interested in developing code that runs two models of dendrite growth into an undercooled melt, generating data linking four variables over a wide range of growth undercoolings and velocities:

- ΔT	Growth undercooling

- V	Tip velocity

- R	Tip radius

- C0	Bulk alloy composition

The LGK model considers dendrite growth into an undercooled melt at velocities where the solid-liquid interface remains at local equilibrium.

The LGK-BCT model considers dendrite growth into an undercooled melt at velocities where rapid solidification effects are significant, including a velocity dependent partition coefficient and velocity dependent liquidus slope.

One further thing…. With the LGK model (the simpler one), it would be very useful if we could use values for k and m that are functions of temperature.  This means that we can use phase diagrams where the liquidus and solidus lines are not straight lines.  Perhaps it would be best if k(T) and m(T) could be entered using a polynomial of order 5.

The LGK model (1984)

Lipton, J., Glicksman, M. E., & Kurz, W. (1984). Dendritic growth into undercooled alloy metals. Materials Science and Engineering, 65(1), 57–63. https://doi.org/10.1016/0025-5416(84)90199-X

∆T=LcpIvt+mC01-11-1-k0Ivc+2ΓR 		(1a)

R=Γσ*PtLcp-PcmC01-k01-1-k0Ivc 					(2a)

With the following identities

Pt=VR2α

Pc=VR2D

Iv(Pt)=PtePtE1(Pt)

Iv(Pc)=PcePcE1(Pc)

Where Pt is the thermal Péclet number, Pc is the solutal Péclet number, Iv(Pt) is the thermal Ivantsov function and Iv(Pc) is the solutal Ivantsov function.

Note that E1(Pc) is the (first) exponential integral of the solutal Péclet number.  In Matlab, the exponential integral of x is written expint(x).

Within these equations, there are eight constant parameters, defined as follows:

L 	Latent heat of fusion. Units: J/kg

cp 	Specific heat capacity.  Units: J/(kg∙K)

m 	Equilibrium liquidus slope. Units: K/ wt.%

k0	Partition coefficient. Unitless

Γ 	Gibbs-Thomson coefficient. Units: K∙m

D 	Solute diffusion coefficient. Units: m2/s

α	Thermal diffusivity in the liquid. Units: m2/s

σ*	Stability constant: Unitless

For Sn-Ag alloys, these parameters are

L= 	61,810.62 J/kg

cp= 	249 J/(kg∙K)

m= 	−3.14 K/ wt.% Ag

k0=	0.0191

Γ= 	8.54*10–8 K m

D= 	1.82E10–9 m2/s

α=	1.5E10–5 m2/s

σ*=	1/(4*(π^2))

There are four variables, defined as follows:

C0 	Bulk alloy composition. Units: wt.%

∆T	Undercooling. Units: K

V 	Velocity. Units: m/s

R 	Dendrite tip radius. Units: m

Fixing two of these variables, the other two can be solved iteratively using a method such as a two-dimensional Newton scheme, also known as the Newton-Raphson method in two variables.

In the codes we have written in the past, the user defines fixed values for C0 and ∆T and the values of the 8 constant parameters.  The code then uses the Newton-Raphson method in two variables to converge on the unique values of V and R that satisfy these two functions. For this, we need to get equations (1a) and (2a) into a form equal to zero and define them as functions f1 and f2:

f1V,R=LcpIvt+mC01-11-1-k0Ivc+2ΓR-∆T=0 	(1b)

f2V,R=Γσ*PtLcp-PcmC01-k01-1-k0Ivc-R=0 					(2b)

The Newton-Raphson scheme in two variables can be written in long form as:

Vn+1Rn+1=VnRn-J-1Vn,Rnf1Vn,Rnf2Vn,Rn

Where n is the current step, n+1 is the next step in the iteration and J is the Jacobian matrix.

J=∂f1∂V∂f1∂R∂f2∂V∂f2∂R

It is convenient to write this in terms of the difference in the variables, ∆V and ∆R

∆V=Vn+1-Vn

∆R=Rn+1-Rn

It is also convenient to have J on the left-hand side so we do not need to use its inverse.

JVn,Rn∆V∆R=-f1Vn,Rnf2Vn,Rn

Which can be written in shorthand as:

J ∆ =- F

∆ can be solved in Matlab with the function ∆ = -J \ F.  Where the backslash operator \ is the matrix left division operator.

Analytical expressions for the partial derivatives for the Jacobian are:

∂f1∂V=LcpdIvtdV-mC01-k0∙dIvcdV1-1-k0Ivc2 						Eq. D2

∂f1∂R=LcpdIvt∂R-mC01-k0∙dIvc∂R1-1-k0Ivc2-2ΓR2 					Eq. E2

∂f2∂V=-Γσ*∙1Q2∙RL2αcp-mC01-k0R1-1-k0Ivc2D-PcmC01-k021-1-k0Ivc2dIvcdV 	Eq. F7

∂f2∂R=-Γσ*∙1Q2∙VL2αcp-mC01-k0V1-1-k0Ivc2D-PcmC01-k021-1-k0Ivc2dIvcdR-1 	Eq. G1

Which include the following

dIvcdV=1+Pc∙ePc∙E1Pc-1∙R2D  		Eq. B2

dIvtdV=1+Pt∙ePt∙E1Pt-1∙R2D 		Eq. B2

dIvcdR=1+Pc∙ePc∙E1Pc-1∙V2D  		Eq. C1

dIvtdR=1+Pt∙ePt∙E1Pt-1∙V2D		Eq. C1

Q=PtLcp-PcmC01-k01-1-k0Ivc							Eq. F1

To perform the Newton-Raphson method, we need an initial guess or approximate solution to the values of V0 and R0, i.e. Vn and Rn when n=0.

The initial guess values can be taken from the approximate analytical solution in Eq. 8.91 and 8.92 of the book ‘Solidification’ by Dantzig & Rappaz (1st Ed) which is only a good approximation (i) at small undercooling, and (ii) for solutal dendrites.

R=6.64π2Γ-m1-k00.25C00.25ΔT1.25

V=D5.51π2-m1-k01.5ΓΔT2.5C01.5

The LKT-BCT model (1987 – 1988)

- Lipton J, Kurz W, Trivedi R. Rapid Dendrite Growth in Undercooled Alloys. Acta Metall. 1987;35(4):957–64.

- W.J. Boettinger, S.R. Coriell, R. Trivedi, Application of dendritic growth theory to the interpretation of rapid solidification microstructures, Rapid Solidif. Process. Princ. Technol. IV (1988) 13.

The equations are written out in simple form in the following papers:

- Appendix to: Sun, S., Li, A., Cheng, C., & Gourlay, C. M. (2025). Effects of Ag and melt undercooling on the microstructure of Sn–Ag solder balls. Journal of Materials Science: Materials in Electronics, 36(942). https://doi.org/10.1007/s10854-025-14979-6

Also..

- Rodriguez, J. E., Kreischer, C., Volkmann, T., & Matson, D. M. (2017). Solidification velocity of undercooled Fe-Co alloys. Acta Materialia, 122, 431–437. https://doi.org/10.1016/j.actamat.2016.09.047

Testing our LGK and our LKT-BCT gives the same result as others…

LGK

- Fig. 3, 4, 5 in Lipton J, Glicksman ME, Kurz W. Dendritic growth into undercooled alloy metals. Mater Sci Eng. 1984 Jul;65(1):57–63.

- Fig. 14 in Boettinger WJ, Bendersky LA, Early JG. An analysis of the microstructure of rapidly solidified Al-8 wt pct Fe powder. Metall Trans A. 1986 May;17: 781–90.

LKT-BCT

- Fig. 2 in Boettinger WJ, Coriell SR, Trivedi R. Application of Dendritic Growth Theory to the Interpretation of Rapid Solidification Microstructures. In: Rapid Solidification Processing: Principles and Technologies IV. 1988. p. 13–25.